## Slide 1: Recent Advances in Antifouling Coatings

## Slide 2: Presentation Content
Introduction
- What is fouling?
- Factors affecting fouling
- Main fouling effects
- Main objective of antifouling
- Challenges
Current antifouling technology
- Biocidal technology
- Non-Biocidal technology
Recent advances
Future challenges

## Slide 3
What is Fouling?
Clean Surface
Conditioning Film
Slime/Biofilm
absorbed organics/minerals
bacteria
microspores/algae
Macro fouling
Plant
Animal
Brown
Red
Green
Soft
Hard
0
1 Min
1 Hr
1 Day
1 Week

## Slide 4: Factors Affecting Fouling
Temperature
Speed/Motion
Light & Nutrients
Water, salinity and pollution
Generally speaking, greatest risk of fouling is with low activity trading extensively in tropical/coastal environments
Vessels at highest risk of fouling when in port (often tropical) while loading/unloading.

## Slide 5: Marine fouling effects
Slime : 1-2% increase in drag
Weed fouling: Up to 10% increase in drag
Shell fouling: Up to 40% increase in drag
Barnacles can cut through coatings
Fouling can grow on top of other fouling

## Slide 6
Barnacles
Barnacles

## Slide 7: Green Weed

## Slide 8: Tube Worms

## Slide 9: Slime

## Slide 10: Fouling can grow on top of other fouling

## Slide 11: Barnacles can cut through Coatings

## Slide 12: Main Objective of A/F Coatings
Preventing the attachment of fouling and hence minimising drag is the main objective of marine antifouling coatings

## Slide 13: Challenges
Ever increasing and unpredictable fuel prices
- Operators are looking at cost more closely than ever
New paint technologies and associated products
- Operators are confused by the claims and counter claims
regarding to A/F
IMO
- Operators have A/F high on the agenda by law
The Environment matters more than ever
- Operators want to be environmentally compliant

## Slide 14: Current Antifouling Technologies
Biocidal technology
Hydration
Hydrolysis Self Polishing Copolymer
Fusion Self Polishing Copolymer
Non-Biocidal technology
Foul Release (non-stick)

## Slide 15: Biocidal Technology – Hydration
Use of Rosin, or derivatives, in the biocide releasing mechanism via “hydration”
Leached layers can become thick- increasing roughness (~75μm)
Higher volume solids content (55-60%)
Film integrity is generally poor, and re-blasting is needed after 10 years
But they are “value for money” for use in lower fouling areas or for vessels with short dry-docking intervals (up to 36 months)

## Slide 16
Section of Hydration
Seawater side
Hull side
Inactive Layer
AF Film (White)

## Slide 17: Shortcomings in Hydration Technology
Coating is reliable upto 3 years only
The dissolution gradually slows down because of a leached layer formed by insoluble materials at the surface.
Hull roughness of surface and fuel consumption will increase with time.

## Slide 18: Biocidal Technology – Hydrolysis
Controlled chemical dissolution (“hydrolysis”) of the paint film presents thin leached layers (10-15 μm)
Therefore long dry-docking intervals (up to 60 months) and better smoothing
Superior overcoatability
Fouling control in outfitting.

## Slide 19
Hydrolysis Mechanism
Seawater
Paint Film
Biocide
Dissolved
Biocide
Hydrolyzing
Polymer
Hydrolyzed
Polymer
Reaction layer
Hydrophobic
resin
Hydrophilic
resin

## Slide 20
Section of Hydrolysis
Seawater side
Hull side
Reaction Layer
AF Film (White)

## Slide 21: Further addition in Hydrolysis Technology
Copper free A/F

## Slide 22
Features- Copper Free A/F
Anti discoloration for outfitting period/copper free tech.
Suitable for application on aluminum boats.

## Slide 23
Copper free – After 12 months
Copper based AF – after 8 months

## Slide 24: Shortcomings in Hydrolysis Technology
Solid content is less, hence coverage is low.
Higher cost.

## Slide 25: Biocidal Technology – Fusion Self Polishing Co Polymer (SPC)
Biocide releasing technology is a mixture of “hydrolysis” and “hydration” mechanisms, combining SPC acrylic polymer with a certain amount Rosin.
Reasonable leached layer thickness (25-30 μm)

## Slide 26
Biocide
Release controller
Hydrophobic resin
Hydrolysis resin
Fusion Self Polishing Mechanism

## Slide 27
Sea Water
Reaction
Biocide
Release controller
Hydrophobic resin
Hydrolysis resin

## Slide 28
Sea Water
Reaction
Biocide
Release controller
Hydrophobic resin
Hydrolysis resin

## Slide 29
Biocidal technology - Summary
“Self-Polishing Copolymer”
Hydrolysis
Fusion
SPC
Hydration
PERFORMANCE
PRICE

## Slide 30: Non-biocidal technology – Foul Release
Silicon based coating
No biocide and hence no leaching
Function by preventing or reducing the adhesion (“non-stick”) of fouling organism
Rely on the movement of the vessel to remove fouling by shear

## Slide 31
Foul Release Coatings – Features & Benefits
Antifouling Performance
Foul Release
Durable & Long lasting
Potential fuel savings and lower emissions
No biocides
Low VOC
Reduce coats
Ultra smooth surface
Lower M&R costs
Keeps fouling off

## Slide 32: How Do Non Stick Coatings Work?
Wa = Yl [1 +COS θ ]
YOUNG-DUPRE Equation
Yl– surface tension of liquid
Wa—adhesion property of liquid against solid surface
θ ---theta-angle of contact
COS θ = COS 180 Degree

## Slide 33
Containers, LNG’s, Tankers
Biocide free coating in Pics

## Slide 34
After 32 months in service

## Slide 35: Recent Advances
Advanced Silyl Technology

## Slide 36: Features
“Advanced” Silyl Technology
Excellent self-polishing Performance
Excellent Static Performance
Silyl Technology
Special Release Controller
Low Friction, Fuel Saving
“Micro” pigmentation & Special resin Technology
Easy Release
Excellent Anti-Fouling Performance
Ultra Smooth Surface (Low roughness & Long wavelength)
Controlled low polishing rate = Reduction of DFT

## Slide 37: Friction Resistance Measurement
Number of Rotation (rpm)
Torque (N・m)
SILYL
8% Reduction of Friction Resistance

## Slide 40: Future Challenges
There is a continual drive to develop improved antifouling coating technologies that will have less environmental impact
•Reduction in fuel consumption
•Release of biocides
The development cycle for new antifouling technologies is relatively long
Considerable formulation work required to meet antifouling performance, mechanical and application property requirements

## Slide 41: Future Advances
Natural Product Antifoulants (NPA’S).
Surface Engineering.
Nanotechnology.
Fluoro Polymers.

## Slide 42
Thank You

## Slide 43
Questions?