## Slide 1
Satish Ogale
Department of Physics and Centre for Energy Science
IISER Pune
satishogale@iiserpune.ac.in, satishogale@gmail.com in
Funding : CSIR, MNRE, DST (Nanomission), DIT, BRNS (DAE), Govt of India
Towards Clean Transportation Through Materials Innovation

## Slide 2
Development
Industrialization
(Energy)
Air and Water Pollution
(Environment)
Health Hazards
https://en.wikipedia.org/wiki/Pollution (references therein)
Ursachen&Auswirkungen.svg
Excessive use of Polluting Fuels

## Slide 3
Distributed
Power
Grid Power

## Slide 5
TRANSPORTATION
&
POLLUTION

## Slide 11
Conversion
Solar Cells, Solar Water Splitting for Hydrogen
Storage
Super-capacitor, Li- Battery
Hybrid Devices
Conservation
Solid State Lighting (LED)
Metal Oxides, Sulfides, Semiconductor QDs
Hybrid Perovskites
Dyes, Functional Polymers,
Ionic liquids, gels, organo-metallics
Functional High Surface Area Carbon, Metal Oxides/sulfides, Conducting Polymers, Engineered Hetero-junction systems and Interfaces

## Slide 12
Gold nanoparticles of different sizes
Passivated Carbon Nanodots
Sun et al. JACS 128, 7756 (2006)
Nanoscience
Quantum Phenomena
Large Surface to Volume Ratio

## Slide 13
Electrical Energy Storage
Stationary Storage For
Renewable Sources
Mobile Storage Storage For
Clean Transportation

## Slide 14
1859: The Lead battery is invented
1887: The first full-scale electric car

## Slide 16
High Energy Density, Moderate Power Density
High Power Density, Moderate Energy Density

## Slide 17
Functional Carbon
Natural Abundance
Diversity of Forms and Functions
Biocompatibility
Conductivity
Surface Area
Porosity
Functionalization
Doping and Defects
Flexibility
Inertness / Reactivity
Dimensionality
Light weight
Molecular
Polymeric
Liquids
Solid
SP2
SP3

## Slide 18
Theranostics 2012; 2(3):235-237
Bulk forms of Carbon;
Introduction to different varieties of Carbon
Nano Carbons Forms
Berchell T.D
Nano Engineered Bulk Carbons
Hard Carbons
Activated Hard Carbons
Soft Carbons
Reprinted and modified with permission of
Elsevier@ Fuels publication

## Slide 19
Raman
Surface area
1730m2/g
ChemSusChem 5, 2159, 2012

## Slide 21
Neem Tree
Neem dead leaves
Crushed powder
Carbon after high
temperature pyrolysis
Supercapacitor from dead leaves carbon
6, 1249, 2013

## Slide 25
Schematic illustration of the synthesis of hard carbon from Walnut shell

## Slide 27
In the News

## Slide 28
In the News

## Slide 30
US Patents Granted from NCL

## Slide 31
High surface area conducting carbon from
Sugarcane Bagasse
Putting scotch tapes on both
sides of Al foil to manage the thickness
Spreading the slurry and
blade coating
Blade coated carbon film
on Al foil
Making a large area supercapacitor electrode

## Slide 32
Contacts made using Al strips
After Rolling with Separator
Electrolyte addition in the glove box
Final sealed supercapacitor

## Slide 33
Electrode Dimensions : Length = 46 cm ,Width= 5cm Total area of the electrode = 230cm2,
Total carbon loading on single electrode ~ 2.5g
Expected Capacitance for the device ~ 100 ± 10 F
Capacitance at 0.1 A ~ 98 F

## Slide 34
KPIT– IISER-P Joint Project
Sodium-ion Battery Development
Team IISERP
Anil Suryawanshi
Dhanya Puthussery
Abhik Banerjee
Yogesh Gawli
Vinita Ahuja
Varun Natu
Team KPIT
Tejas Kashtriya
Sarika Phadke
Anil Suryawanshi
Kauthubh Phathak
Abhay Patwardhan
Nagaraj
KPIT Retrofitted Electric Bus

## Slide 35
Use Case: Inter-city public transportation bus, 9 meter-11 Ton
Daily running ~200 km, average route distance < 25 km
Fast-charging batteries solutions  20 min top-up charging at the end of every trip  1/3rd capacity pack on-board (600 kgs)
Half cell testing done up to 6000+ cycles at 2C/8C
Full cell testing done up to 6000+ cycles at 2C/8C
Current  Pouch cell fabrication and optimization

## Slide 36
Sun, Water and Hydrogen

## Slide 42
Dye Sensitized Solar Cells & Perovskite Solar Cells
Devices are certified at IIT Bombay
Champion Conversion Efficiency > 22%

## Slide 43
Dye sensitized solar cell (DSSC) by a novel fully room temperature process: a solar paint for smart windows and flexible substrates
RSC Advances, 2012, 2, 11645–11649

## Slide 44
Small Scale Applications

## Slide 45
Functional Nanomaterials and Interface systems for
Sensor Applications
Sensors
Functional Soft Materials
Photo-sensors, Touch/Pressure Sensors
Nanogenerators

## Slide 46
Advanced Sensors (IOT-Internet of things)
Driverless Car

## Slide 48
Wearable
Self-powered
or
Low Power
Light weight
Robust
Water /Dust Resistant
Heat resistant
New Generation Devices

## Slide 51
FE SEM
TEM

## Slide 52
Fe3O4 – Carbon magnetically recoverable high surface area
Super-absorbant nanocomposites

## Slide 54
Using Gels as Nanocatalyst Support

## Slide 55
Sl.No | Metals(5ppm) | % Removal | 
 |  | Sabja | Fe3O4 -Sabja
1 | As+3 | 53.32 | 98
2 | Cr+3 | 69.40 | 96
3 | Cr+6 | 55.32 | 86
4 | Pb+2 | 44.11 | 92
5 | Cd+2 | 32.35 | 84
6 | Hg+2 | 40.16 | 90

## Slide 56
Dip Coating
Spray Pyrolysis
Screen Printing
Multi-Coating system
Hot Roll Press
Device fabrication facilities @ NCL
TiO2 blocking layer deposition
TiO2 mesoporous layer deposition
Mesoporous TiO2 films
Spray pyrolysis system useful for uniform blocking layer on large area (10cm X 10cm)
Programmable hot plate
Laser scriber

## Slide 57
Large area DSSC fabrication
Silver and UV sealant dispensing robotic arm
Silver fingers for efficient charge collection
Silver line/UV sealant width in micron scale
UV irradiation chamber
Electrode pile up machine
DSSC device (7 cm X 7 cm)

## Slide 58
Solar Simulator
Sideways Solar Simulator
Impedance measurement
Transient Absorption set up
(Developed in-House)
IPCE measurement set up
Solar Cell characterization facilities @ NCL

## Slide 59
Material synthesis and device fabrication for charge storage systems
Tube furnace maximum temperature 13000C
Electrospinning System
High speed centrifuge

## Slide 60
Material synthesis and device fabrication for charge storage systems
Multi-Coating system
Hot Roll Press
Punching & crimping machines
Hydraulic press
Mixing machine

## Slide 61
Electrochemical work-station
Battery testing systems with 8 channels
Device characterization of charge storage systems
Autolab Potentiostat

## Slide 62
Sputtering/ Evaporator
Glove box
Thickness Profilometer
FE-SEM
Other device fabrication facilities & Characterization facilities @ NCL
Excimer laser λ=248nm
Deposition chamber
Pulsed laser deposition system
Gas chromatography machine

## Slide 63
The Team
Next Generation Solar Cells, Solar Fuels, Charge Storage
Photovoltaics and Advanced Semiconductor Characterization
Theory
And Predictive Modeling
Molecular & Mesoporous Materials, MOFs, COFs
Electrochemistry, Charge storage Devices, Fuel Cells
Quantum Dots
and
Photophysics
Plasmonics and Photonics
Growth and Properties of Novel Materials
Satish Ogale
Shouvik Datta
Mukul Kabir
R. Vaidhyanathan
Musthafa Muhammed
Angshuman Nag
Pavan Kumar
Surjeet Singh

## Slide 64
Background
Dye Cell
2D Perovskite Nanostructures
Solar Water Splitting
Plasmonics
Supercapacitor
LED/QLED/OLED
COF electrocatalyst Water Splitting
Perovskite Cell 16.8%
Dye Cell 9%

## Slide 67
It is all in our hands
Thank You