## Slide 1
EUGENE FONSECA
SATEJ JOSHI
AMEY PESHWE
REDUCTION OF SHIP WEIGHT
USING ALUMINIUM FOAM

## Slide 2: AIM
Reduction in Ship Structural Weight.
Improving Cargo Carrying Capacity.
Adhering to Environmental Standards.

## Slide 3
SIMPLY SUPPORTED BEAM
19.65 Kg

## Slide 5
UNDER UTILIZED
Chart: Density
| Density Kg/m3
Steel | 7850
Aluminum | 2712
New Material | 500
Water | 1000
STEEL
STEEL
LIGHT WEIGHT
MATERIAL

## Slide 6
ALUMINIUM FOAM
METAL FOAM
Excellent Energy Absorption
Low Thermal Conductivity
Sound and Vibration Damping and Absorption
Tailorable Density
Recyclable
ALUMINIUM
VOID SPACES

## Slide 7
STEEL
STEEL
ALUMINIUM
FOAM

## Slide 8: STEEL VS SAS SANDWICH
Chart: 
| Steel Plate (11mm) | SAS (24mm)
Weight(Kg) | 4.12 | 4.12
Stress(MPa) | 16.46 | 13.04
Deflection(mm) | 1.528 | 1.133

## Slide 9
Sandwich
Steel

## Slide 12
AlSi12
TiH2
Precursor
MANUFACTURING

## Slide 13
BONDING

## Slide 14: COMPLEX STRUCTURES

## Slide 15
FORGING
Complex Structures from SAS sandwiches, forged
in a die.
Forging reforms the foam structure resulting in
densification of the foam core.
Densification improves impact absorption

## Slide 16
WELDING
The method of welding used is pulse beam welding.
Pulse beam welding employs mili-second long pulses to join two SAS panels.

## Slide 18
CORROSION TEST
:Results: Aluminium Foam is unaffected by the corrosive medium (sea water) and no structural defects were detected. Steel face sheets are protected by usual anti corrosive methods. Al Foam Sandwich is suitable for marine use.
Aluminium Foam Exposed to NaCl
spray for 1000 hours.

## Slide 20
APPLICATION
Vessel : MV Derbyshire
Biggest British Ship lost in Typhoon on 10.09.1980 at 4 years age.
:Vessel Particulars:
Length: 281.94 Meters.
Beam: 44.20 Meters.
Depth: 24.90 Meters.
Construction Date: 1976
Vessel Type: (OBO) Carrier
Number of Cargo Holds: 9
Class: DNV
Hatch Cover
Faulkner’s improved design single skin, transversely stiffened type.

## Slide 21
FAULKNER’S DESIGN
Transverse Stiffener | Input
Top flange breadth (b) | 63 cm
Top flange thickness (t) | 1.05 cm
Web height (h) | 63.5 cm
Web thickness (t) | 1.5 cm
Bottom flange breadth (b) | 28 cm
Bottom flange thickness (t) | 2.5 cm
Neutral Axis (z) | 33.4 cm
Design Load | 17.5 kN

## Slide 22
Chart: OPTIMISATION
| STEEL: 10MM FOAM: 100MM | STEEL: 10MM FOAM: 130MM | STEEL: 10MM FOAM: 150MM | STEEL: 9MM FOAM: 150MM | STEEL: 8MM FOAM: 150MM
THICKNESS (MM) | 110 | 140 | 160 | 159 | 158
WEIGHT (MT) | 43.26 | 46.41 | 48.51 | 45.23 | 41.95
MAX STRESS (Mpa) | 42 | 34.36 | 30.402 | 31.2654 | 32.5787
DEFLECTION (MM) | 38.261 | 31.032 | 27.263 | 28.07 | 29.29
SAS DESIGN
Proposed Design

## Slide 23
FEM ANALYSIS
Faulkner’s Hatch Cover:
Max Stress : 109 MPa
SAS Panel Hatch Cover:
Max Stress : 32 MPa

## Slide 24
Chart: THICKNESS
| Thickness (mm)
FAULKNER'S DESIGN | 670
IMPROVED DESIGN | 168
Chart: WEIGHT
| WEIGHT (MT)
FAULKNER'S DESIGN | 76.887
IMPROVED DESIGN | 41.958
Chart: DEFLECTION
| Deflection (mm)
FAULKNER'S DESIGN | 3.664
IMPROVED DESIGN | 2.929
Chart: MAX STRESS
| Max Stress(MPa)
FAULKNER'S DESIGN | 92.3609
IMPROVED DESIGN | 32.5787
75.2%
70.1%
20%

## Slide 25
FEM - RESULTS
Parameter | Steel Hatch Cover | (SAS) Hatch Cover
Thickness | 670 mm with 14 stiffeners | 150 mm Al Foam with 8 mm Face Steel Sheet
Weight | 76.887 MT | 41.958 MT
Deflection | 3.664 mm | 2.929 mm
Max Stress | 109.36 Mpa | 32.58 MPa

## Slide 26
Chart: COST
| US Dollars
FAULKNER'S DESIGN | 51188.68
IMPROVED DESIGN | 123519.2

## Slide 27
Chart: RECOVERY TIME
| 15 | 30 | 45 | 60 | 75 | 90 | 105 | 120
Additional investment | 650979 | 650979 | 650979 | 650979 | 650979 | 650979 | 650979 | 650979
Saving | 108675 | 217350 | 326025 | 434700 | 543375 | 652050 | 760725 | 869400
Saving of 315 Ton for 9 hatch covers together.
The freight charges for shipping iron ore : 23 USD/tonnes.
Thus the total profit achieved in every voyage is: 315 x 23 = 7245 USD
The additional cost for using SAS design amounts to 72,331 USD
Voyages to break even : 87

## Slide 28: CONCLUSION
The FEM results along with our experiments conclusively satisfy our aim and prove that SAS is a smart material and a viable alternative to steel in the future.

## Slide 29: FUTURE WORK

## Slide 30: Acknowledgements
Any project idea requires authenticated inputs based on well-rounded research. A lot of data and research work was provided to us by Fraunhofer Institute for Machine tools and Forming Technology, based in Chemnitz, Germany through their Head of the Department, Dr. THOMAS HIPKE. This invaluable support is greatly acknowledged.
We sincerely thank the following for their key inputs and guidance: Mr. AYAZ KHAN, Cdr. BHASKAR WALIMBE Dr. SANJAY POHEKAR Dr. SANJEET KANUNGO Mr. INDRA BASU Mr. SHISHIR DUTT Mr. ARUN MAHAJAN Mr. AMOL TATKE All the instructors in TMI workshop for helping prepare the model.

## Slide 31: THANK YOU! ANY QUESTIONS?